Supporting Information

A self-assembled nanoflower-like Ni5P4@NiSe2 heterostructure with hierarchical pores triggering high-efficiency electrocatalysis for Li-O2 batteries

Xue Han1, Yanjie Liang1, Lanling Zhao2, Jun Wang 1,*, Qing Xia1, Deyuan Li1, Yao Liu1,*, Zhaorui Zhou1, Yuxin Long1, Yebing Li1, Yiming Zhang1, Shulei Chou3,*

1 Key Laboratory for Liquid-Solid Structural Evolution and Processing of Materials (Ministry of Education), Shandong University, Jinan 250061, China

E-mail: jw707@sdu.edu.cn; liuyao@sdu.edu.cn

2School of Physics, Shandong University, Jinan 250061, China

3Institute for Carbon Neutralization, College of Chemistry and Materials Engineering

Wenzhou University, Wenzhou 325035, China

E-mail: chou@wzu.edu.cn

Figure S1. Fabrication photograph of Ni5P4@NiSe2 heterostructure.

Figure S2. XRD pattern of Ni(OH)2 precursor.

Figure S3. SEM images of Ni(OH)2 precursor.

Figure S4. SEM images of Ni5P4 sample.

Figure S5. SEM images of NiSe2 sample.

Figure S6. The atomic ratios of Ni5P4 and NiSe2 by XPS, EDS and ICP testing.

Figure S7. The battery testing box purchased from NJZH (Shenzhen) Scientific Ltd.

Figure S8. Initial discharge/charge plots of carbon paper.

Figure S9. Initial discharge/charge profiles of KB cathodes at different current densities.

Figure S10. XRD pattern of pure carbon paper.

Figure S11. The Li2O2 formation and decomposition mechanism on Ni5P4@NiSe2 cathode.

Table S1. Electrocatalytic activity comparison of Ni5P4/NiSe2 cathodes with those of the recently reported similar cathodes.

| Catalysts | Morphology | Discharge Capacity mA g-1/mA g-1 | Cycle number (cycles/cutoff Capacity) | Ref. |
| --- | --- | --- | --- | --- |
| FeSe | Hollow spheroids | 14273/500 | 130/1000 | 1 |
| Ni2P/Ni12P5@NF | honeycomb-like | 13254.1/500 | 125/1000 | 2 |
| NiSe2@NiO | hierarchical | 11512/500 | 90/1000 | 3 |
| Ni12P5/RuO2/C | nanoparticles | 4296/200 | 56/500 | 4 |
| Ni2P | nanoparticles | 4104.4/200 | 70/500 | 5 |
| Co-Ni2P | 3D umbrella-like | 9331/100 | 147/1000 | 6 |
| Ni5P4@NiSe2 | Nanoflower-like | 19090/100 | 202/600 | This work |

[1] Yoo H, Lee G H and Kim D W 2021 J. Alloys Compd. 856 158269

[2] Ran Z Q,  Shu C Z, Hou Z Q, Zhang W B, Yan Y, He M and Long J P 2021 Chem. Eng. J. 413 127404

[3] Wen X J, Ran Z Q, Zheng R X, Du D Y, Zhao C, Li R J, Xu H Y, Zeng T and Shu C Z 2022 J. Alloys Compd. 901 163703

[4] Wang S Z, Hu J W, Gui X F, Lin S D and Tu Y Y 2021 Solid State Ion 372 115773

[5] Ran Z Q, Shu C Z, Hou Z Q, Hei P, Yang T S, Liang R X, Li J B and Long J P 2020 Electrochim. Acta 337 135295

[6] Hou Z Q, Shu C Z, Hei P, Yang T S, Zheng R X, Ran Z Q and Long J P 2020 Nanoscale 12 6785-6794